SP 400		ASPHALT CONCRETE SURFACING

(1-15-25)

I.	Description

- Materials

A.	Asphalt

B.	Joint Filler

C.	Aggregate

D.	Mineral Filler

E.	Preparation of Mineral Aggregates

F.	Preparation and Composition of Mixtures

G.	Formula for Job Mix

H.	Field Laboratory

I.	Samples for Tests

- Construction Methods

A.	Asphalt Plant

B.	SP 407 Tack Coat

C.	Control of Asphalt Concrete Surfaces

D.	Transportation of Mixtures

E.	Placing of Mixtures

F.	Constructing Longitudinal & Transverse Joints

G.	Compaction of Mixtures

H.	Protection of Pavement

I.	Tolerance in Pavement Thickness, Compaction 	and Finished Surface

- Reclaimed Asphalt Pavement (RAP)

A.	Removal

B.	Stockpiling

C.	Material Breakdown

D.	Preparation of Mineral Aggregates

E.	Preparation and Composition of Mixtures

- Method of Measurement

VI.	Basis of Payment

VII.	Price Adjustment – Asphalt Binder Material

SP 400		ASPHALT CONCRETE SURFACING

Items 302, 407 and 408 of the Specifications are hereby deleted and the following (including references to SP302, SP402, SP403, SP404, and SP407) substituted therefore:

I.	Description

This Work shall consist of furnishing, mixing, placing, and compacting asphalt concrete base, 	intermediate and surface courses over an existing pavement base or prepared aggregate base in accordance with these Special Provisions and in accordance with the lines, grades, sections, and dimensions as shown on the Plans.  The thickness of asphalt courses shall be as indicated on the Plans, unless otherwise directed by the Chief Engineer.

# II.	Materials

# A.	Asphalt

All asphalt materials shall conform to the requirements for the respective grades specified below as shown in the following tables for each grade. Liquid asphalts shall not foam when heated to the specified application temperature.

(Tables Following)

# AASHTO DESIGNATION: MP 1

Table 1. Performance Graded Asphalt Binder Specification

SP 400 – ASPHALT CONCRETE SURFACING							3 of 28

Performance Grade	PG 46	PG 52	PG 58                                		PG 64

-34-     -40      -46	-10    -16    -22   -28    -34   -40    -46	-16       -22        -28      -34      -40	   -10      	-16      -22       -28     -34     -40

# Average 7-day Maximum Pavement

Design Temperature, C a	<46	<52		<58		<64

# Minimum Pavement

Design Temperature, C a	                    >-34     >-40    >-46	          >-l0  >-16  >-22  >-28  >-34  >-40   >-46 	  >-16    >-22     >-28    >-34    >-40 	>-l0   >-16    >-22    >-28    >-34    >-40

# Original Binder

Flash Point Temp, T48: Minimum C				230

# Viscosity, ASTM D 4402: b

Maximum, 3 Pas (3000 cP),

Test Temp, C				135

Dynamic Shear, TP5:

# G*/sin , Minimum, 1.00 kPa

Test Temperature @ 10 rad/s, C	46	52		58		64

# Rolling Thin Film Oven (T 240) or Thin Film Oven (T 179) Residue

Mass Loss, Maximum, %				1.00

Dynamic Shear, TP5:

# G'/sin 8, Minimum, 2.20 kPa

Test Temp @ 10 rad/sec, C	46	52		58		64

Pressure Aging Vessel Residue (PP1)

PAV Aging Temperature, C	90	90		100		100

Dynamic Shear, TP5:

# G*sin , Maximum, 5000 kPa

Test Temp @ 10 rad/sec, C		10       7        4	        25   22   19   16    13     10      7	25     22     19     16     13		31    28    25    22    19    16

Physical Hardening e			Report

# Creep Stiffness, TPl: f

S, Maximum, 300 MPa

m-value, Minimum, 0.300

Test Temp, @ 60 sec, C                                     -24    -30    -36          	 0   -6   -12  -18   -24   -30   -36      	-6    -12    -18    -24    -30                 	0      -6    -12    -18     -24    -30

Direct Tension, TP3: f

Failure Strain, Minimum, 1.0%

Test Temp @ 1.0 mm/min, C           -24    -30    -36 		 0   -6   -12   -18   -24   -30  -36	 -6   -12   -18    -24    -30		0  -6  -12 -18 -24 -30

# AASHTO DESIGNATION: MP 1

# Table 1. Performance Grade Asphalt Binder Specification

SP 400 – ASPHALT CONCRETE SURFACING							 4 of 28

Performance Grade	PG 70	PG 76	PG 82

-10 -16 -22 -28 -34  -40	-10 -16  -22 -28 -34 	-10 -16 -22 -28  -34

# Average 7-day Maximum Pavement

Design Temperature, C 	<70	<76	<82

Minimum Pavement Design

Temperature, C                                       	>-10 >-16 >-22 >-28 >-34>-40 	>-l0 >-16  >-22 >-28  >-34  	 >-10 >-16 >-22 >-28 >-34

# Original Binder

Flash Point Temp, T48: Minimum C		230

Viscosity, ASTM D 4402: 1)

Maximum, 3 Pa-s (3000 cP),		135

Test Temp, C

# Dynamic Shear, TP5: C

G*/sin , Minimum, 1 .00 kPa	70	76	82

Test Temperature @ 10 rad/s, C

# Rolling Thin Film Oven (T 240) or Thin Film Oven (T 179) Residue

Mass Loss, Maximum, %		1.00

Dynamic Shear, TP5:

G*/sin , Minimum, 2.20 kPa	70	76	82

Test Temp @ 10 rad/sec, C

# Pressure Aging Vessel Residue (PP1)

PAV Aging Temperature, C	100(110)	100(110)	100(110)

Dynamic Shear, TP5:

G*sin , Maximum, 5000 kPa	34       31      28     25      22     19	37       34      31       28      22	40     37	34    31	28

Test Temp @ 10 rad/,sec, C

Physical Hardening e		Report

# Creep Stiffness, TP1: f

S, Maximum, 300 MPa

m-value, Minimum, 0.300	0       -6     -12    -18    -24     -30	0   -6   -12    -18     -24	0   -6   -12    -18    -24

Test Temp, @ 60 sec, C

Direct Tension, TP3: t

Failure Strain, Minimum, 1.0%	0      -6      -12     -18   -24     -30	0   -6   -12    -18     -24	0   -6    -12   -18    -24

Test Temp @ 1.0 mm/min, C

SP 400 – ASPHALT CONCRETE SURFACING							 5 of 28

NOTES:

a.      	Pavement temperatures can be estimated from air temperatures using an algorithm contained in the Superpave software program or may be provided by the specifying agency, or by following the procedures as outlined in PPX.

b.       	This requirement may be waived at the discretion of the specifying agency if the supplier warrants that the asphalt binder can be adequately pumped and mixed at temperatures that meet all applicable safety standards.

c.       	For quality control of unmodified asphalt cement production, measurement of the viscosity of the original asphalt cement may be substituted for dynamic shear measurements of G*/sin  at test temperatures where the asphalt is a Newtonian fluid.  Any suitable standard means of viscosity measurement may be used, including capillary or rotational viscometer (AASHTO T201 or T202).

d.       	The PAV aging temperature is based on simulated climatic conditions and is one (1) of three (3) temperatures ninety (90)C, 100C or 110C.  The PAV aging temperature is 100C for PG 64 and above, except in desert climates, where it is 110C.

e.      	Physical Hardening - TP 1 is performed on a set of asphalt beams according to Section 13.1 of TP 1, except the conditioning time is extended to twenty-four (24) hours ± ten (10) minutes at ten (10)C above the minimum performance temperature.  The twenty-four (24) hour stiffness and m-value are reported for information purposes only.

f.       	If the creep stiffness is below 300 MPa, the direct tension test is not required.  If the creep stiffness is between 300 and 600 MPa the direct tension failure strain requirement can be used in lieu of the creep stiffness requirement.  The m-value requirement must be satisfied in both cases.

SP 400 – ASPHALT CONCRETE SURFACING						 6 OF 28

# Rapid-Curing (RC) Liquid Asphalts

AASHTO	ASTM

CHARACTERISTICS				Test	     	Test	   		       		 GRADES

Method		Method	  	 RC-70	 RC-250	       RC-800	     RC-3000

Kinematic Viscosity at 140oF., cs.	 		T201	     	D2170	  	 70-140	 250-500	    800-1600	   3000-6000

Flash Point (Open Tag) oF.		 		T79	     	D1310	  		        80+	             80+	              80+

# Distillation

Distillate (per cent of total

distillate to 680oF.)

to 374oF.			 	     		  		       10+	    .........	         .........	          .........

to 437oF.			 	T78	     	D402	  	       50+	       35+	            15+	          .........

to 500oF.			 	     		  		       70+	       60+	            45+	             25+

to 600oF.			 	     		  		       85+	       80+	            75+	             70+

Residue from distillation to 680oF.,

per cent by volume			 	     		  		       55+	       65+	            75+	             80+

Tests on Residue from distillation:

Penetration, 77oF., 100 g., 5 sec.	 		T49	     	D5		  80-120	  80-120	       80-120	        80-120

Ductility, 77oF., cms.		 		T51	     	D113	  	     100+	     100+	          100+	           100+

Solubility in Carbon Tetrachloride	 		T44	     	D4		    99.5+	    99.5+	         99.5+	          99.5+

Water, % 				 	T55	     		  	      0.2-	      0.2-	           0.2-	            0.2-

SP 400 – ASPHALT CONCRETE SURFACING 						7 OF 28

Medium Curing (MC) Liquid Asphalts

AASHTO	ASTM

CHARACTERISTICS	     		Test	  	Test	     			   	GRADES

Method		Method     	MC-30	       MC-70       MC-250       MC-800       MC-3000

Kinematic Viscosity at 140oF., cs.     		T201	  	D2170	     	  30-60	        70-140       250-500      800-1600     3000-6000

Flash Point (Open Tag)  oF.	       		T79	  	D1310	     	   100+	           100+	 150+	     150+             150+

Distillation -

Distillate (per cent of total

distillate

to 680oF.

to 437oF.		       		  	     			     25-		 20-	       0-10	  .........            .........

to 500oF.		       		T78	  	D402	     	 40-70	         20-60	     15-55	     35-	           	    15-

to 600oF.		       		  	     			 75-93	         85-90	     60-67	 45-80      	15-75

Residue from distillation to 680oF.,

per cent by volume		       		  	     			    50+		55+	        67+	    75+	       	   80+

Tests on Residue from Distillation:

Penetration, 77oF., 100 g., 5 sec.   			T49	  	D5	         120-250	     120-250	 120-250       120-250         120-250

Ductility, 77oF., cms.	       			T51	  	D113	     	  100+	          100+	      100+	  	100+        100+

Solubility in Carbon

Tetrachloride, %		       		T44	  	D4	            99.5+	         99.5+	     99.5+          99.5+              99.5+

Water, % 			       		T55	  	D95	      	  0.2-	           0.2-	       0.2-	   	0.2-             0.2-

SP 400 – ASPHALT CONCRETE SURFACING 						8 OF 28

Slow-Curing (SC) Liquid Asphalts

AASHTO	ASTM

CHARACTERISTICS			Test	     	Test	   		      		GRADES

Method		Method	 	  SC-70		SC-250		SC-800		SC-3000

Kinematic Viscosity at 140oF., cs.	 		T201	     	D2170	  	  70-140     	 250-500	 	800-1600	3000-6000

Flash Point (Cleveland Open Cup), oF.		T48	     	D92	  	   150+	  	 175+	               200+	    	      225+

Distillation:

# Total Distillate to 680oF., % by

Volume 				 	T78	     	D402	  	    10-30	  	  4-20	      	    2-12	    	           5-

# Float Test on Distillation Residue

at 122oF., sec.			 		T50	     	D139	  	  20-100		25-110	      	50-140	    	   75-200

Asphalt Residue of 100 Penetration, %		T56	     	D243	  	       50+	   	  60+	      	     70+	    	        80+

Ductility of 100 Penetration Asphalt

Residue at 77oF., cms.		 		T51	     	D113	  	     100+	   	100+	      	   100+	    	      100+

Solubility in Carbon Tetrachloride, %	 	T44	     	D4		    99.5+	 	 99.5+	             99.5+	    	     99.5+

Water, % 				 	T55	     	D95	  	      0.5-	   	 0.5-	      	   0.5-	    	       0.5-

SP 400 – ASPHALT CONCRETE SURFACING 						9 OF 28

Emulsified Asphalts

AASHTO	ASTM	     			  	GRADES

CHARACTERISTICS	       	Test	  	Test	         	       Rapid            		Medium	 	        Slow

Method		Method        	      Setting         	  	Setting        	       Setting

RS-1	    RS-2	  	MS-2	    	SS-1         SS-1h

CSS-1      CSS-1h

# TEST ON EMULSION

Fural Viscosity at 77oF., sec.       		 	     		         20-100	   .........	  	100+	         20-100       20-100

Fural Viscosity at 122oF., sec.      		  	     				  75-400

Residue from Distillation, % by

weight 			       		  	     			    57	       62+	    	62+	              57+            57+

Settlement, 5 days, difference       		  	     			    3-	         3-	      	3-	                3-	           3-

Demulsibility:

35 ml. of 0.02 N CaC12	       		  	     		  60+	       50+	  	........	     	........           ........

50 ml. of 0.10 N CaC12	       		  	     		........	     ........	      	30	     	........           ........

Sieve Test (Retained on No. 20)      	  	     			 0.10	      0.10	   	0.10	     	0.10-            0.10

Cement Mixing Test		   	  	     			........	     ........	  	........	     	  2.0-              2.0

# TEST ON RESIDUE

Penetration 77oF., 100g., 5 sec.     		T49	  	D5	       100-200	 100-200       	100-200        100-200   	      40-90

Solubility in Carbon Tetrachloride   	T44	  	D4	           97.5+	 97.5+		97.5+	           97.5+               97.5+

Ductility 77oF., cms.		   	T51	  	D113	     	40+	  40+		  40+	           40+                 40+

1.	Asphalt Binders shall conform to the Performance Graded Asphalt Binder Specifications of AASHTO Designation MP1.  Binder grades shall be as shown in the Plans. Each initial job mix formula (“JMF”) submittal shall include a letter of certification (and all dated MP1 data) from the asphalt binder supplier stating compliance with AASHTO Designation MP1 and the Force Ratio (“FR”) requirements of each binder grade.  These letters of certification are mandatory for acceptance of the JMF by the testing laboratory.  Any change in binder or polymer source will require a new JMF and letters of certification.

(a)	In addition to the requirements of AASHTO Designation MP1, the Force Ratio for the specified binders shall be:

|  | 64-22 | 70-22 (FR) | 76-22 (FR) |
| --- | --- | --- | --- |
| Force Ratio, f2/f1, (min.) |  | 0.30 | 0.35 |

FR Denotes asphalt, which meets Force Ratio requirements.

- FR is not applicable

The FR is defined as the force at thirty (30) cm elongation (f2) divided by the maximum force at the initial peak (f1) when the asphalt binder is tested in accordance with AASHTO T-300 with the following conditions and modifications:

(b)	The testing temperature shall be 39.2oF.

(c)	The rate of travel shall be five (5) cm/min.

The FR requirements shall be obtained through modification of a non-oxidized, virgin asphalt binder by adding a styrene butadiene styrene polymer block copolymer (“SBS polymer”).  All virgin asphalt binders shall not contain any reclaimed products or portions of reclaimed products that were originally developed and marketed for another end use (i.e., motor oil or motor oil bottoms from reclamation).

- All SBS polymer modification shall be performed prior to shipment to the hot mix facility (pre-blend).

The supplier of a polymer modified binder shall give the Contractor for each Project a handling guide specifying temperature, circulation, shelf life and other requirements for assuring the polymer modified binder will perform as desired.  This handling guide will be provided to the Chief Engineer, Testing Lab and plant control room.  If polymer modified binder is retained at the hot mix facility for more than two (2) weeks before use or beyond the supplier recommended shelf life, whichever is less, a Separation of Polymer Test or top and bottom sample test shall be performed by the Testing Lab on samples retrieved by the Contractor at the Testing Lab’s direction and the binder shall not be used until approved.

- Liquid Asphalt Cutback shall be RC-70, RC-250, MC-30 or MC-70, or RC-800 or RC-3000.

4.	Emulsified Asphalt shall be SS-1 or RS-2.

# B.	Joint Filler

1.	Hot applied joint sealer shall conform to Section 705.04 of the Specifications.

2.	Cold joint filler:

(a)	Material shall conform to the requirements of the effective editions of the following Specifications.

(1)	Federal Specifications SS-R-406C

(2)	ASTM D95-99

(3)	ASTM D147-41 (1965)

(4)  	ASTM D217-97

(b)  	Composition of the material shall meet the following minimum requirements:

(1)	Not less that 5.5 percent rubber.  The successful bidder shall submit notarized certifications stating the quantity of styrene-based virgin synthetic rubber contained in the sealing compound supplied under this Special Provision.

(2)	Not more than thirty-four (34) percent filler.

(3)	Not less than forty-five (45) percent solids (other than inert fillers).

(4)	Not more than three (3) percent water.

(5)	There shall be no separation or settling of the sealer when exposed to temperature of 120oF for seventy-two (72) hours in a closed box, 2.75 inches in diameter and two (2) inches deep.

C.	Aggregate

1.	Aggregate for base course and leveling courses shall conform to the requirements of Section 703.05 of the Specifications, except as modified herein.

(a)	Coarse aggregate shall consist of crushed carbonate stone or crushed air-cooled blast furnace slag, whichever is preferred by the Contractor. Open hearth furnace slag, basic oxygen furnace slag and electric furnace slag (steel slags) shall be prohibited.

2.	Aggregate for surface course shall conform to the requirements of Section 703.05 of the Specifications, except as modified herein.

(a)	Fine aggregate for asphalt concrete mixtures containing slag or limestone coarse aggregate, as indicated in the Plans and Bid Form, shall be composed primarily of natural sand with the blending of manufactured sand (703.05) allowed only if necessary to achieve the VMA and/or F/T values.  If the sand is manufactured from gravel, it shall be crushed from gravel material retained on the 3/8 inch sieve.

Natural sand shall consist of hard, sharp, angular grains of quartz or other hard, durable rock, free from lumps of clay, loam, coatings of any injurious materials or other foreign matter.  Dune sand, beach sand, or sand having smooth rounded surfaces shall not be used.

(b)	Coarse aggregate shall consist of crushed carbonate stone or crushed air-cooled blast furnace slag, as indicated in the Plans and Bid Form. Open hearth furnace slag, basic oxygen furnace slag and electric furnace slag (steel slags) shall be prohibited.

D.	Mineral Filler

The mineral filler shall consist of limestone dust, dolomite dust, or Portland cement and shall be free from foreign or other objectionable material.  It shall be dry and free from lumps and when tested by means of laboratory sieves, the mineral filler shall meet the following gradation requirements:

Percent

Passing No. 30 sieve			    	   100

Total Passing No. 100 sieve, not less than	     85

Total Passing No. 200 sieve, not less than	     65

# E.	Preparation of Mineral Aggregates

The aggregate shall be dried and delivered to the mixer at a temperature necessary to achieve a proper mix temperature as specified in this Special Provision.

# F.	Preparation and Composition of Mixtures

1.	The composition of the mixture shall conform to the requirements hereinafter stated.  The fraction actually retained between any two consecutive sieves shall not be less than four (4) percent, except that between sieves No. 30 and No. 80 it shall be not less than three (3) percent, and between sieves No. 80 and No. 200 shall be not less than two (2) percent.  The percentage passing the No. 200 mesh screen is inclusive of any mineral dust present in the refined asphalt.

2.	After the ingredients have been properly proportioned and introduced into the mixer, mixing shall be continued for a period necessary to produce a homogeneous mix of thoroughly coated aggregate.  All mixing shall be done in conformance with Section 401 of the Specifications.

# GRADATION OF TOTAL AGGREGATE

Percent Passing by Weight

| Sieve Designation | SP 402 Intermediate Course Asphalt | SP 404 Surface Course Asphalt | SP 403 Leveling Course Asphalt | SP 302 Asphalt Base |
| --- | --- | --- | --- | --- |
| 2 inch | -- | -- | -- | 100 |
| 1½ inch | -- | -- | -- | 85-100 |
| 1 inch | 95-100 | -- | -- | 68-88 |
| ¾ inch | 85-100 | -- | -- | 56-80 |
| ½ inch | 65-85 | 100 | 100 | 44-68 |
| 3/8 inch | -- | 80-98 | 80-100 | 37-60 |
| No. 4 | 35-60 | 50-75 | 50-75 | 22-45 |
| No. 6 | -- | 40-65 | 40-65 | -- |
| No. 8 | 25-48 | 30-55 | 30-55 | 14-35 |
| No. 16 | 16-36 | 22-42 | 22-42 | 8-25 |
| No. 30 | 12-30 | 14-30 | 14-30 | 6-18 |
| No. 50 | 5-18 | 6-20 | 6-20 | 4-13 |
| No. 100 | 2-10 | 4-15 | 4-15 | -- |
| No. 200 | -- | 2-8 | 2-8 | 2-6 |
| Asphalt Binder Content by Weight | 4.0% to 9.0% | 4.5% to 9.5% | 4.5% to 9.5% | 3.0% to 8.0% |
| Fines to Effective AC Ratio | 1.1 Max. | 1.1 Max. | 1.1 Max. | 1.5 Max. |
| *F/T Value (Percentage Points Max.) | +2 | +2 | +2 | -- |

* The value (calculated to the nearest percentage point) of the Fifty (50) to Thirty (30) (F/T) value shall be defined as the percent of total aggregate retained between the No. 50 and No. 30 Sieves, minus the percent of total aggregate retained between the No. 30 and No. 16 Sieves, up to plus four (4) percentage points for the production mix.

G.	Formula for Job Mix

1.	The general composition limits prescribed above are master ranges of tolerances to govern mixtures made from any raw materials meeting Specification requirements, and they are maximum and minimum for all cases.  A job mix formula (JMF) will be required as a closer control appropriate to the job materials incorporated into the mixtures furnished by the Contractor.  Before any paving is begun, the Contractor shall submit to the Chief Engineer a job mix formula for use in determining what proportions the proposed aggregates should be combined to produce a mix in compliance with these Specifications.  No Work shall be started until the Contractor has submitted and received approval of the plant formula.  The Contractor must concur with the recommended approval by the testing laboratory before final approval by the Chief Engineer.

The submission of such job mix formula shall, upon approval and thereafter, bind the Contractor to furnish paving mixtures not only within the above master ranges, but as a further requirement, also meet the exact formula thus set up for the Project within the following tolerance allowances.

Optimum asphalt percentages for the job mix formula shall be developed from the five (5) point Marshall Air Void Curve using 3.8 percent air void for surface course and four (4.0) percent for base course.  Optimum asphalt content will be based on mix being oven cured one (1) hour to simulate travel and lay down time prior to compaction.

Tolerance for SP 302 asphalt base:

Passing maximum sieve size

down to 3/8 inch sieve...............……	±7%

Passing No. 4 sieve.......................…±6%

Bitumen............................................	±0.3%

Tolerance for SP 402 base course:

Passing maximum sieve size

down to 3/8 inch sieve......................	±7%

Passing No. 4 sieve..........................	±6%

Passing Nos. 6 and 50 sieves..........	±4%

Bitumen............................................	±0.3%

Tolerance for SP 404 surface course and SP 403 leveling course:

Passing maximum sieve size

down to 3/8 inch sieve.....................	±5%

(not to exceed 98%)

Passing No. 4 sieve.........................	±5%

Passing Nos. 6, 8, 16, 30, 50 &

100 sieves........................................	±3%

(#30 not to exceed 30%)

Bitumen............................................	±0.3%

In addition to the above gradation and tolerance requirements, the JMF and production material is to have no more than three (3) percent upward deviation below Sieve No. 4 and above Sieve No. 100; measured from a straight line drawn from the origin of the 0.45 power grading chart to the point at which the gradation crosses the No. 4 Sieve.

Sampling:

Extraction/Gradation - Every   500T of Daily Production

Marshall Properties   - Every  1000T of Daily Production

Samples of the completed mixture shall be analyzed at least once daily or more frequently as directed by the Chief Engineer.  Stability testing during production will not be required if the design stability exceeded 2,000 lbs.  Sampling of any or all combinations of fine and coarse aggregate shall be accomplished at the cold elevator at least once daily and at the hot bins as required.  As long as there is no change in the gradation of the material in the bins, it will not be necessary to change the formula at the mixer.  If, however, there is a decided change in the grading of the aggregates so that the composition of the mix is falling outside the Specification limits, then the entire mix must be recomputed and the formula at the mixer changed accordingly.

2.	After the proper combination of aggregates and asphaltic cement have been developed, the mix shall be tested for stability and density in accordance with the standard Marshall Stability Tests in accordance with AASHTO T245-97, except that test specimens shall be compacted by seventy-five (75) blows.

The asphalt concrete base course, intermediate course, surface course and the leveling course shall meet the following requirements:

| Characteristics | Values | Values |
| --- | --- | --- |
|  | SP 402, SP 403, SP 404 | # SP 302 |
| Stability (lbs.) | 1800 Min. | 3000 Min. |
| Flow (0.01 in.) | 8 – 14 | 28 Max. |
| Voids (%) | 3 - 5 | 3 - 8 |
| Voids in Mineral Aggregate (%) - Surface & Base Course (3/8" max. size aggregate)* | 15 Min. | -- |
| Voids in Mineral Aggregate (%) -- Base Course (3/4" max. size aggregate)* | 13 Min. | -- |
| Voids in Mineral Aggregate (%) -- Asphalt concrete Base Course (2" max. size aggregate)* | -- | 11.5 Min. |
| Density of Laboratory Compacted Mixture in Percent of Calculated Voidless Mixture of Same Material | 95 – 97 | 92-97 |
| Compacted Field Density in Percent of In-Situ Voids.( Calculated from a Voidless Mixture) | 3.0 to 8.0 | 3.0 to 8.0 |
| Percent Voids Filled with Asphalt (VFA) | 65 Min. - 75 Max. | 65 Min. - 75 Max. |

* Base on maximum size aggregate in mix.

In addition, the asphalt cement mix shall be subjected to the immersion-compression test, AASHTO Designation T-165, and the Index of Retained Strength (wet-dry ratio) shall be not less than seventy-five (75).  This test shall be made for each aggregate source and at such intervals as the Chief Engineer may direct. Subject to the approval of the Chief Engineer, hydrated lime or a chemical additive may be used as required to obtain the required Index of Retained Strength.

H.	Field Laboratory

The Contractor shall provide, for each mixing plant, a Level 2 field laboratory that is in compliance with Ohio Department of Transportation (ODOT) Supplement 1041, Asphalt Concrete Program Administration.  All ODOT approvals and certifications shall be submitted to the Chief Engineer for review and acceptance.

The cost of furnishing the laboratory and equipment shall be included in the Contract unit prices bid for the various items of asphaltic concrete courses.  The equipment shall remain the property of the Contractor after completion of the Project.

I.	Samples for Tests

1.	Pavement Samples

Each day during construction, testing laboratory personnel shall cut from the course of compacted mixture, as directed by the Chief Engineer, at least one (1) sample of each day’s Work, but not less than one (1) sample for each 4,000 square yards of pavement course constructed which shall be taken to the laboratory for examination and tests.  The location from which each sample is taken shall be accurately identified.  Samples shall be carefully cut from the pavement and, when cooled, packed for transportation so that they will not deform.  Either a four (4) inch core (SP 402, SP 403, SP404), a six (6) inch core (SP 302), or a rectangular block sample may be taken.  The area of pavement so removed shall be replaced by the Contractor with new mixture and refinished as directed by the Chief Engineer.  No additional compensation will be allowed for replacing the areas with new pavement.

2.	Samples of Mixture

Unless otherwise directed, the completed mixture shall be sampled once daily for Max. Specific Gravity ASTM D-2041, extraction and Marshall properties, and more frequently if required.  Samples for daily extraction are to be taken by trained plant personnel under close observation of the Chief Engineer.  Samples for other tests required under these Specifications shall be taken by the Chief Engineer.

3. 	Compaction Density Samples

Core samples shall be cut from each day's compacted course.  A minimum of one (1) core for every 1,000 linear lane feet shall be cut and tested for compaction and thickness.

4.	Samples of Asphalt Binder

Random samples of the asphalt binders shall be taken by the Contractor throughout the Project as directed by the Chief Engineer.  These samples shall be taken while under the supervision of the testing laboratory.  The testing laboratory shall certify that the asphalt binder meets the performance graded Asphalt Binder Specifications of AASHTO Designation MP1 and the specified FR requirements.

# III.	Construction Methods

A.	Asphalt Plant

All asphalt concrete mixing plants used by the Contractor for the preparation of asphalt paving mixtures shall conform to all requirements of Section 402 of the Specifications, except as modified herein.  They shall be fully automated, including automatically printed delivery tickets, so designed and operated to produce a mixture within the job mix tolerances as provided for in these Specifications.    The Chief Engineer or its authorized representatives shall at any time have access to all parts of the Asphaltplant to ensure the manufacturing process of the Asphalt Concrete mixture is in strict accordance with the Specifications.  The asphalt concrete mixing plant or plants which the Contractor uses shall have adequate capacity to meet all requirements of the time schedule specified for the Project and to deliver on a continuous basis adequate quantities of asphalt concrete to the number and type of paving machines specified for the paving operation.  Supply of asphalt concrete for mainline Work shall be from one (1) plant only, unless otherwise approved by the Chief Engineer.  If a second plant is approved, the delivery shall be limited to a specific paving lane for each plant.

In the event that the plant or equipment fails to operate properly, it shall be shut down until such time as any or all deficiencies are corrected.

The Contractor shall furnish a list of the equipment available and assigned for use on this Work and a certification as to the plants and their daily tonnage that will be assigned and used on this Project as per Article 14, Submittals.

While supplying Ohio Turnpike Projects, the Contractor will not make any changes in the plant screens or weights without permission of the Chief Engineer.

The Contractor shall maintain at all times a stockpile sufficient to complete a minimum of one (1) week's Work.  This stockpile must be tested and approved by the Chief Engineer, or his dually appointed representative, prior to its being used.  Materials shall not be added to stockpiles in use.  Materials stored in adjacent stockpiles shall be kept separated and adequate partitions shall be provided between stockpiles when necessary to accomplish this.

B.  	SP 407 Tack Coat

Tack Coat supplied for the Work shall conform to all applicable portions of ODOT Item 407 for the Plan specified materials.

C.	Control of Asphalt Concrete Surfaces

1.	All asphalt concrete paving equipment shall be in accordance with all applicable portions of 401.03, and 401.08.

2.	In the event of failure of any of the automatic grade and cross slope controls or their components on the paver or of the profile grade reference system being used, the Contractor will be permitted to operate by manual control only until all hot mixed material then in transit is in place but no longer than forty-five (45) minutes, after which time paving operations shall be discontinued until all equipment is again in good working order.

3.	Automatic controls may be omitted on pavers used on interchange and service plaza ramps.

4.	Profile grade control for the asphalt resurfacing of the traffic lanes shall be the centerline of the existing pavement, or either the right or left edges of the existing pavement, or any combination of these that may be required.

D.	Transportation of Mixtures

1.  	Transportation of asphalt concrete to the Work site shall be in accordance with all applicable portions of 401.03 and 401.07.

2.	Each load of asphalt concrete mixture delivered from the plant to the site of the Work shall be accompanied by a delivery ticket carried by the truck driver from the plant inspector to the inspector on the site of the Work.  The blank forms for the delivery tickets shall be furnished in duplicate by the Contractor.  Delivery tickets for each load shall be distinguished by a serial identification number and shall also show the following additional information:

The date and time at which the load leaves the plant; the identification number of the truck; the temperature of the mixture; the JMF number; product name with PG grade; and the written signature of the plant inspector as an indication of its acceptance of material.

One (1) copy of each ticket shall be kept by the plant inspector and the copy sent out with the haul truck shall be kept by the inspector at the site of the Work.  Any truck load of asphalt concrete mixture arriving at the site of Work without a properly signed delivery ticket shall be rejected and removed from the site of the Work.

3.	Trucks that drip petroleum products on the asphalt concrete surface under construction shall be repaired immediately or removed from the Work site and Turnpike right-of-way until rendered satisfactory for return by the Chief Engineer.

4.	The Contractor's vehicles shall maintain a minimum speed of fifty (50) MPH outside of the construction area.

E.	Placing of Mixtures

- Pre-Placement Meeting

Prior to the commencement of the paving operations, a pre-placement meeting shall be held at the Project site.  Those attending the pre-placement meeting shall include but not limited to the Contractor, its paving superintendent and other qualified paving supervisor(s), and the Chief Engineer.  The Contractor shall submit an outline of the qualifications and experience of the Contractor’s paving superintendent and paving supervisor(s) to the Chief Engineer for approval within ten (10) days of the Notice to proceed

The topics to be discussed at the pre-placement meeting shall include, but not be limited to, the following:

- Review of placement procedures.

- Review of Equipment submittals.

- Requirements for pavement smoothness/ acceptability.

- Review of batch plant procedures.

- Review of testing procedures.

- Requirements of personnel.

- Traffic and safety considerations.

- Placement Temperature

The temperature of the asphalt concrete mixtures at the time of placement shall be as follows unless otherwise recommended by the Performance Grade (“PG”) binder manufacturer:

# Minimum Laydown Temperature (ºF)

| Surface Temp. (ºF) | Minimum Lift Thickness (inches) |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | ½ | ¾ | 1 | 1½ | 2 | 3 or more |
| 20-32 | -- | -- | -- | -- | -- | 285 |
| 32-40 | -- | -- | -- | 305 | 295 | 280 |
| 40-50 | -- | -- | 310 | 300 | 285 | 275 |
| 50-60 | -- | 310 | 300 | 295 | 280 | 270 |
| 60-70 | 310 | 300 | 290 | 285 | 275 | 265 |
| 70-80 | 300 | 290 | 285 | 280 | 270 | 265 |
| 80-90 | 290 | 280 | 275 | 270 | 265 | 260 |
| 90 or higher | 280 | 275 | 270 | 265 | 260 | 255 |

The Chief Engineer may request an increase in the above minimum temperatures should high wind conditions cause rapid heat dissipation.

- Asphalt Placement

Unless otherwise specifically permitted by the Chief Engineer, all asphalt concrete mixtures for base and surface courses shall be spread and finished by self-powered and propelled mechanical finishing machines meeting the following requirements:

(a)	Mechanical finishers shall have a capacity of at least 500 tons per eight (8) hour day and shall have a forward and reverse traveling speed of not less than 100 feet per minute; shall be equipped with a quick and efficient steering device; and shall be capable of laying the asphalt concrete mixture true to the line, grade, and cross section shown on the Plans.  When laying mixtures, the finisher shall operate at a speed between five (5) and forty-five (45) feet per minute, as may be directed by the Chief Engineer.

(b)	The spreading and finishing equipment shall be equipped with hoppers, distributing screws and a positive, controlled mechanical floating screed.  The screed shall be equipped with a suitably controlled heating device to be used when conditions require its use to obtain the desired texture.  The mixture shall be dumped in the center of the hoppers and care shall be exercised to avoid overloading and slopping over the mixtures upon the base.  The term "screed" includes any "strike-off" device operated by cutting, crowding, or other practical action which is effective on the mixture without tearing, shoving or gouging and which produces a finished surface of the evenness, smoothness, and texture specified.  The screed shall be adjustable and have automatic leveling control as specified in paragraph III.E.3.(c).

(c)	Finishers shall employ mechanical or other compensating devices to adjust the grade and confine the edges of the mixture to true lines without the use of stationary side forms.  They shall be capable of spreading the mixtures without segregation, in the thickness of from three-quarter (3/4) inch to at least three (3) inches, to a maximum width of not less than fourteen (14) feet, and of adjustment to spread the mixture in strips of less than fourteen (14) feet in width, in steps of one (1) foot or less, to a minimum width of eight (8) feet.

(d)	Courses requiring beveled edges shall be laid with pavers equipped with bevel end plates.

(e)	Finishing machines shall be constructed and operated so that material does not accumulate and remain along the sides of the receiving hopper where it cools off and is unfit for use and must be removed.

(f)	Finishers that drip petroleum products on asphaltic concrete surfaces under construction shall be repaired immediately or removed from the Work site and the Turnpike right-of-way until rendered satisfactory for return by the Chief Engineer.

- A leveling course is provided to remove irregularities in the pavement and to re-establish the profile at approaches to structures.

- The SP 404 shall be laid either in full width of the pavement as shown in the Plans or in two (2) parallel lanes.

If laid full width, the paving machine shall be equipped with automatic grade and cross slope control devices equivalent to the devices specified under paragraph III.C.1.  The machine used for this purpose need not be adjustable to the widths required under III.E.3.(c) for other machines required for narrower paving.

If laid in two (2) parallel lanes, the longitudinal joints between the lanes shall be at the exact locations of the longitudinal joints in the Portland cement pavement.  The lanes shall be laid simultaneously by pavers operating in parallel, and no individual lane shall be advanced more than 100 feet ahead of the adjacent lane.  The rate that the asphalt concrete mixture is laid and rolled shall be coordinated so that a hot, well compacted, dense longitudinal joint is obtained at all times.

The Contractor shall maintain sufficient stand-by equipment to continue normal paving operations in the event any paving machine does not properly perform or produce pavement meeting the requirements of the Specifications so that the paving Work may be properly prosecuted without appreciable delay to the Work.

- A Material transfer device (MTD) shall be used for all course(s) of mainline and ramp paving including SP404, SP402 and SP302.  The MTD shall be self-propelled and independent of the asphalt spreading and finishing equipment.  The MTD shall be capable of remixing and transferring the asphalt mixture from the MTD to the asphalt spreading and finishing equipment.

MTD may be used for shoulder paving but is not required.

4.	The surface of curbs and gutters in actual contact with asphaltic mixtures shall be painted with a thin uniform coating of asphaltic cement to provide a closely bonded watertight joint at these points.  After completion of the surface course, the joint shall be sealed by applying asphaltic cement in a uniform width of approximately four (4) inches and at a rate just sufficient to fill surface voids.

5.	Immediately after the asphalt concrete mixture for any course has been laid by the paver and before roller compaction is started, the surface shall be checked, any inequalities adjusted, sandy accumulation from the screed removed by rake or hoe, and all fat or segregated spots in any course removed and replaced with satisfactory material.  Irregularities in the surface and alignment along the outside edges of base courses shall be corrected by the addition or removal of mixture before the edge is rolled.  The Contractor shall provide competent workmen and supervisors who are capable of performing the Work incidental to correcting of all pavement irregularities.  Special attention shall be given by him to the straight-edging of each course before completion of the rolling in order to minimize subsequent corrections in the surface course, as required by SP 400S.

6.	Mixtures may be spread by hand only upon permission by the Chief Engineer and at such locations as are inaccessible to machine spreading.  They shall then be handled and spread by means of heated shovels, lutes, and rakes. Mixtures shall not be applied faster than they can be properly handled and spread.  Workmen shall not stand or Work in the hot mixture while it is being placed, and every precaution shall be taken to distribute and spread the material uniformly to avoid segregation of the coarse aggregate and asphalt binder.

7.	Pavement under construction, which becomes contaminated by petroleum products shall be removed and replaced at the Contractor's expense.

8.	In areas where pavement settlement, for a distance greater than thirty-five (35) feet, has occurred and more than one (1) layer of leveling course will be required to obtain the original pavement grade, the Contractor shall use automatic leveling control devices as directed by the Chief Engineer.  The Contractor shall use a taut wire set to profile grade for the profile control sensor to follow on each layer to insure that the constructed leveling course restores the original pavement grade prior to placing of the base course.

9.	Compacted depths of any one (1) layer of asphalt concrete shall meet the following requirements:

SP 302..............................4 Min. - 8 Max. (Place in 2 equal lifts when required thickness exceeds 8.)

SP 402.............................3 Max.

SP 403 & SP 404..............2 Max.

F.	Constructing Longitudinal and Transverse Joints

- General

Joints shall be constructed as per Section 401.08.D of the Specifications and as amended in this Special Provision.

2.  	Longitudinal Joints

The longitudinal joints in the surface course shall be made in a careful manner by skilled workmen.  The asphalt concrete being placed in the abutting lane shall be tightly crowded against the vertical face of the previously placed lane.  The finishing machine shall be positioned so that in spreading, the material overlaps the edge of the lane previously placed by one (1) to two (2) inches.  The machine must closely follow the line or marking placed along the joint for this purpose.  Prior to rolling, the coarse aggregate in the material overlapping the joint shall then be carefully broomed, luted or raked onto the surface of the unrolled lane.  This leaves only the fine portion of the mixture, which will be pressed into the compacted lane at the time the joint is rolled.  The brooming, luting or raking shall be done directly after the material has been spread by the finishing machine.  A steel wheel roller shall be used for the initial rolling. The roller being used should be shifted over onto the previously placed lane so that no more than six (6) inches of the rear roller wheel rides on the edge of the fine material left by brooming, luting or raking.  The roller shall continue to roll along this line, shifting its position gradually across the joint in approximately six (6) inch increments until a thoroughly compacted, neat joint is obtained.  Only short sections shall be left where the abutting lane is not placed the same day.  Where the abutting lane is not placed or the joint is distorted during the day's Work by traffic or from any other cause, the edge of the lane shall be carefully trimmed to line and painted with a very thin coat of asphalt cement before the abutting lane is placed.

3.  	Transverse Joints

Transverse joints in all courses shall be carefully constructed and thoroughly compacted to provide a smooth riding surface over these joints in the pavement.  Joints shall be straight edged and string lined to assure this quality. For surface courses, construct transverse joint on a 6:1 skew perpendicular to the centerline of the lanes.  For intermediate and base courses, transverse joints may be constructed perpendicular.  Joints may be sawed or bulk headed.  If a bulkhead is used and the roller is permitted to roll over the end of the new material, the line of joint shall be trimmed back of the rounded edge a sufficient distance to provide a true surface and cross section.  The face of the joint shall be painted with a thin coating of asphalt cement before placing fresh material against it.  To obtain thorough compaction, and at the direction of the Chief Engineer, cross rolling may be required at these joints.  Cross rolling shall be required at all approach slabs.

G.  	Compaction of Mixtures

1.	Rolling to obtain consolidation and compaction of the base course and surface course shall start as soon as possible after the material is spread by the finishing machine.  It is imperative that most of the rolling be done while the material is at its most favorable temperature, which is directly after spreading. Rolling shall be continued until there is no movement or marking of the material under the roller wheels and until the specified compaction has been obtained.  When required, complete transverse and longitudinal rolling and two (2) diagonal rolling, approximately at right angles to each other, shall be performed.

2.	During rolling, the roller wheels shall be kept moist to avoid picking up the material. The use of excess water to accomplish this will not be permitted.  Excess SP 404A placed on the existing pavement surface at the adjacent longitudinal joint shall be removed prior to paving the SP 404 to prevent roller pickup and mat tearing/damage.

3.	Compaction shall be effected with approved tandem power rollers and pneumatic rollers as herein before specified.  A minimum of two (2) steel-wheel rollers shall be used in each lane in conjunction with one (1) pneumatic roller compacting all lanes.  Additional rollers may be ordered by the Chief Engineer should compaction or other conditions so require.

4.	Rolling of normal and superelevated pavement sections shall start at the low side and gradually progress toward the high side of the pavement, overlapping on successive trips by at least one-half (1/2) the width of tandem rollers and uniformly one (l) lapping each preceding track or covering the entire surface with the rear wheel.  Crowned sections shall be rolled in the same manner, except that rolling shall start at the sides and proceed toward the center.  The rollers shall move at a slow but uniform speed (maximum speed three (3) miles per hour), and the line of rolling shall not be suddenly changed or the direction of rolling suddenly reversed. Unsupported edges shall be rolled prior to the remainder of the course. If at any point, particularly where the roller is reversed, rolling causes displacement of the material, the affected areas should be loosened at once with lutes or shovels and restored to the original grade of the loose material before being re-rolled.  Heavy equipment or rollers shall not be permitted to stop/stand on the finished surface, including but not limited to filling up with water and/or fuel, until it has thoroughly cooled.

5.	Rolling shall be a continuous operation.  The first rolling of the freshly laid mixture shall be accomplished by steel-wheel rollers.  Additional rolling shall be completed with steel-wheel rollers and pneumatic tire rollers.  Tandem rollers (twelve (12) to fourteen (14) tons) shall be used for the finish and final rolling.  All rolling operations shall proceed continuously until all roller marks are eliminated and the density of the compacted surface meets the requirements of II.G.2.  The Contractor shall submit its proposed rolling operations and equipment for review and approval by the Chief Engineer.

6.	Along curbs and other locations inaccessible to rollers, the compaction shall be accomplished with mechanical tampers or with hot iron tampers weighing not less than twenty-five (25) pounds and having a bearing area not exceeding forty-eight (48) square inches.  At all contacts of this character, the joints between these structures and the mixture must be effectively sealed.

7.	The Contractor shall provide heating equipment for keeping hand tools free from asphalt.  The temperature of the tools when used, shall not be greater than the temperature of the materials being placed.  Only heat shall be used to clean hand tools; petroleum oils or volatiles shall not be permitted for this purpose.

H.	Protection of Pavement

All vehicular traffic and all construction equipment shall be kept off the freshly compacted sections of base, intermediate and surface courses until the material has cooled sufficiently (140oF maximum surface temperature or otherwise what is necessary to prevent distortion of the surface and to make certain that fines are not removed by "picking-out" from traffic).

I.	Tolerance in Pavement Thickness, Compaction and Finished Surface

It is the Commission's intention to rate the general rideability of the finish surface per SP 400S.  This will be done immediately upon completion of the paving zone with the results determined within fourty-eight (48) hours.  The Contractor's schedule is to reflect this delay as well as any additional time required for any and all corrective work, as the opening of the paved zone to Turnpike traffic will not be permitted pending results per SP 400S.

# IV.	Reclaimed  Asphalt Pavement (RAP)

Reclaimed hot plant-mixed asphalt concrete base (SP 302) and/or asphalt concrete intermediate course (SP 402) may be substituted for the mixture as specified under the following conditions:

A.	Removal

The removal process of the existing asphaltic material, which is to be salvaged for recycling under Item SP 302 or SP 402, shall produce stockpiles of material uniform in gradation and composition.  Removal of the salvaged material for recycling on this portion of the Project shall be by the single-pass cold milling method with or without mechanical crushing as is necessary.

B.	Stockpiling

Salvaged asphaltic concrete material from this Project, which is to be reused in the reclaimed Item SP 302 or SP 402, shall be placed in a separate stockpile at the asphalt plant location.

The areas to be covered by the stockpiled material shall be cleared and prepared to facilitate recovery of the maximum amount of the stockpiled material.  The upper six (6) inches of the area on which the reclaimed pavement is stockpiled shall be free of all clods, lumps or stones exceeding two (2) inches.  The Contractor shall construct the stockpile in such a manner as will limit the compaction of the reclaimed pavement, thus providing expedient recovery and breakdown for introduction into the reclaimed pavement mix.

C.	Material Breakdown

The removed material used for recycling shall be broken down to the extent necessary for proportioning uniformly into the mixing plant and for blending with other specified materials in accordance with the requirements for the completed mixture.  The acceptable nominal maximum size of individual pieces will be governed by these requirements.

D.	Preparation of Mineral Aggregates

1.	Section II.E.  Preparation of Mineral Aggregates will apply with the following modifications:

(a)	Batch plants shall have the means for feeding reclaimed material into the weight box and a device for proportioning and introducing the recycling agent into the mixer.  The temperature of the mixture shall be controlled by the transfer of heat from the new aggregate within the mixer.

(b)	Drum mix plants shall be designed, constructed, and operated for producing reclaimed mixtures with the specified recycling agents.

E.	Preparation and Composition of Mixtures

1.	Section II.F.  Preparation and Composition of Mixtures will apply with the following modifications:

(a)	The specified fractions retained between sieve sizes shall not apply.

2.	If reclaimed mix is furnished, several tons of pavement shall be removed and stockpiled for use in preparing the job-mix formula.  Both the initial job-mix formula and any adjustments must be approved by the Chief Engineer prior to use in production.

3.	The Contractor shall use the salvaged pavement materials obtained from the Project by the single-pass cold milling method (use of any salvaged pavement materials from sources other than the Commission is strictly prohibited) to produce a reclaimed mix containing not less than seventy (70) percent new aggregate for drum mix plants or not less than seventy (70) percent new aggregate for batch type plants.  All reclaimed mixes that have a specified FR requirement shall contain not less than eighty (80) percent new aggregate.  The new and salvaged materials must be blended by means of controlled gates in the plant feeder system.

4.	If reclaimed mix is furnished, an approved recycling agent must be added to the mixture to produce the specified asphalt binder grade of the binder material.

5.	All binders used shall be of the PG specified.  Blending with a lower PG asphalt binder will not be permitted.

# V.   	Method of Measurement

For Pavement Reconstruction projects, new construction, resurfacing and all other asphalt paving projects, the pay quantity of asphalt concrete with specified uniform plan depth will be field verified / calculated using the plan width and measured length along the centerline of the accepted material placed.  Paving in excess of the plan width or plan length is not eligible for pay, unless otherwise approved by the Chief Engineer.

# VI.   	Basis of Payment

The yardage of the asphalt concrete courses will be paid for at the Contract unit price per cubic yard bid for each course, which price and payment shall be full compensation for furnishing, hauling, placing and compacting all materials and for all labor, equipment, tools and incidentals necessary to construct the asphalt concrete course in accordance with the Plans and these Special Provisions.

If a uniform course is specified in the Plans for payment, the Commission will not pay for cubic yards that exceed the quantity calculated from the Plan lines and dimensions, unless approved by the Chief Engineer.

Payment for Tack Coat will be made on the basis of the actual number of gallons used, accepted complete in place.

If the Contractor’s bid is based on providing SP 402 with RAP, and if for any reason the Contractor cannot provide acceptable reclaimed material, Special Provisions SP 402 - Asphalt Concrete Intermediate Course, Using Crushed Stone will be provided in lieu of the RAP at no additional expense to the Commission.

Item	Unit		Description

SP 302	Cu. Yd.	Asphalt Concrete Base, PG______

SP 402	Cu. Yd.     	Asphalt Concrete Intermediate Course, PG

SP 403	Cu. Yd.	Asphalt Concrete Leveling Course, PG_______

SP 404	Cu. Yd.    	Asphalt Concrete Surface Course, Using Crushed Stone, PG ______

SP 404	Cu. Yd.    	Asphalt Concrete Surface Course, Using Crushed Slag, PG ______

SP 407	Gallon	Tack Coat

- Price Adjustment - Asphalt Binder Material

Price adjustment for Asphalt Binder Material shall be in accordance with SP 118 of the Specifications.

Price adjustments will be calculated and applied as soon as practical after the completion of the Project. The following materials, if used, will be subject to price adjustment, regardless of method of measurement:

SP 302, SP 402, SP 403, SP 404, SP 407